Contents

1. Purpose	2

2. Input files	2

2.1. parameter.system.in	2

2.2. parameter.atom.in	2

2.3. phaseFra.in (optional)	3

2.4. displace.in (optional)	3

2.5. strucOrd.in (optional)	4

2.6. region.in (optional)	4

3. Output files	5

References	5

Diffraction Documentation

# 1. Purpose

The Q-POP-Diffraction module computes the diffraction pattern of a material microstructure predicted by phase-field simulations. It takes inputs of

(1) crystal cell and atomic information and

(2) the real-space microstructure data described by the spatial distributions of phases, structural orders, and mechanical displacements that are generated by phase-field simulations,

and outputs the corresponding diffraction intensity distribution in the reciprocal space.

Formalism of the diffraction computation can be found in Ref. [1].

# 2. Input files

The input of the program consists of 2 required input files including parameter.system.in and parameter.atom.in, and 4 optional input files including phaseFra.in, displace.in, strucOrd.in, and region.in. The choice of optional input file(s) to be provided depends on the type of the system considered.

## 2.1. parameter.system.in

Declares the size of the system and the number of phases. The format is as follows:

Table 1 Format of the input file parameter.system.in

| Data in the file |  |  | Explanation |
| --- | --- | --- | --- |
|  |  |  | Comment or empty line |
| l1 | l2 | l3 | System size in each direction (in nm) |
| n1 | n2 | n3 | Total number of simulation grids in each direction |
| ns | nf |  | Thickness of the substrate and the film (in grid numbers). For a bulk system, put ns = nf = 0. |
|  |  |  | Comment or empty line |
| N |  |  | Total number of phases |
| H |  |  | Total number oof structural order parameters |
|  |  |  | Comment or empty line |
| ε11 | ε22 | ε33 | Average mechanical strain of the system |
| ε23 | ε13 | ε12 |  |

## 2.2. parameter.atom.in

Declares the crystal cell and atomic information. The format is as follows:

Table 2 Format of the input file parameter.atom.in

| Data in the file |  |  | Explanation |  |
| --- | --- | --- | --- | --- |
|  |  |  | Comment or empty line |  |
| q10 | q20 | q30 | Reciprocal lattice point around which the diffraction pattern will be calculated (nm−1) |  |
| a1 | a2 | a3 | Lattice parameter a of an unstrained unit cell (nm) |  |
| b1 | b2 | b3 | Lattice parameter b of an unstrained unit cell (nm) |  |
| c1 | c2 | c3 | Lattice parameter c of an unstrained unit cell (nm) |  |
| N |  |  | Number of atoms in a unit cell |  |
|  |  |  | Comment or empty line |  |
| ΔRn,1 | ΔRn,2 | ΔRn,3 | Coordinates of the n-th atom in a unit cell (unitless). This line repeats N times, in the sequence of n=1,2,…,N. |  |
|  |  |  | Comment or empty line |  |
| m |  |  | Phase identifier (ID) | This part further repeats M times, in the sequence of m=1,2,…,M. Each repetition provides the information of one phase. |
| fn,m (real) | fn,m (imag) |  | Atomic form factor of the n-th atom in a unit cell of the m-th phase, real and imaginary parts (unitless). This line repeats N times, in the sequence of n=1,2,…,N. |  |
| bn,m,h,1 | bn,m,h,2 | bn,m,h,3 | Atomic-displacement-over-order-parameter coefficient bn,m,h of the n-th atom over the h-th order parameter, in the m-th phase. This line repeats N×H times, in the sequence of (n,h)=(1,1),(1,2),…,(1,H),(2,1),…,(2,H),…,(N,H). This line is removed if H=0. |  |

We recommend the X-ray database from Lawrence Berkeley National Laboratory (  https://henke.lbl.gov/optical_constants/asf.html) [2] for atomic form factors.

## 2.3. phaseFra.in (optional)

Stores an array of the spatial distribution of phase fraction ηmr (unitless) arranged in a row-major order, where m is the phase ID with m=1,2,...,M. This file should be provided for systems with multiple phases that have different chemical compositions (M≥2). It can be obtained from phase-field simulations. The format is as follows:

Table 3 Format of the input file phaseFra.in

| Data in the file |  |  |  |  |  |  | Explanation |
| --- | --- | --- | --- | --- | --- | --- | --- |
| n1 | n2 | n3 |  |  |  |  | Total number of simulation grids in each direction |
| 1 | 1 | 1 | η11,1,1 | η21,1,1 | … | ηM1,1,1 | Phase fraction ηm of the m-th phase (m=1,2,…,M) at grid point (1,1,1) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| 1 | 1 | n3 | η11,1,n3 | η21,1,n3 | … | ηM1,1,n3 | Phase fraction ηm of the m-th phase (m=1,2,…,M) at grid point (1,1,n3) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| 1 | n2 | n3 | η11,n2,n3 | η21,n2,n3 | … | ηM1,n2,n3 | Phase fraction ηm of the m-th phase (m=1,2,…,M) at grid point (1,n2,n3) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| n1 | n2 | n3 | η1n1,n2,n3 | η2n1,n2,n3 | … | ηMn1,n2,n3 | Phase fraction ηm of the m-th phase (m=1,2,…,M) at grid point (n1, n2, n3) |

## 2.4. displace.in (optional)

Stores an array of the spatial distribution of mechanical displacement ur (unit: nm) arranged in a row-major order. This file should be provided for systems that show strong mechanical deformations. It can be obtained from phase-field simulations. The format is as follows:

Table 4 Format of the input file displace.in

| Data in the file |  |  |  |  |  | Explanation |
| --- | --- | --- | --- | --- | --- | --- |
| n1 | n2 | n3 |  |  |  | Total number of simulation grids in each direction |
| 1 | 1 | 1 | u11,1,1 | u21,1,1 | u31,1,1 | Displacement u at grid point (1,1,1) |
| ⋮ |  |  |  |  |  | ⋮ |
| 1 | 1 | n3 | u11,1,n3 | u21,1,n3 | u31,1,n3 | Displacement u at grid point (1,1,n3) |
| ⋮ |  |  |  |  |  | ⋮ |
| 1 | n2 | n3 | u11,n2,n3 | u21,n2,n3 | u31,n2,n3 | Displacement u at grid point (1,n2,n3) |
| ⋮ |  |  |  |  |  | ⋮ |
| n1 | n2 | n3 | u1n1,n2,n3 | u2n1,n2,n3 | u3n1,n2,n3 | Displacement u at grid point (n1, n2, n3) |

## 2.5. strucOrd.in (optional)

Stores an array of the spatial distribution of structural order parameter ζhr (unitless) arranged in a row-major order, where h is the structural order parameter ID with h=1,2,...,H. This file should be provided for systems possessing structural orders (H≥1). It can be obtained from phase-field simulations. The format is as follows:

Table 5 Format of the input file strucOrd.in

| Data in the file |  |  |  |  |  |  | Explanation |
| --- | --- | --- | --- | --- | --- | --- | --- |
| n1 | n2 | n3 |  |  |  |  | Total number of simulation grids in each direction |
| 1 | 1 | 1 | ζ11,1,1 | ζ21,1,1 | … | ζH1,1,1 | Value of the h-th order parameter ζh (h=1,2,...,H) at grid point (1,1,1) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| 1 | 1 | n3 | ζ11,1,n3 | ζ21,1,n3 | … | ζH1,1,n3 | Value of the h-th order parameter ζh (h=1,2,...,H) at grid point (1,1,n3) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| 1 | n2 | n3 | ζ11,n2,n3 | ζ21,n2,n3 | … | ζH1,n2,n3 | Value of the h-th order parameter ζh (h=1,2,...,H) at grid point (1,n2,n3) |
| ⋮ |  |  |  |  |  |  | ⋮ |
| n1 | n2 | n3 | ζ1n1,n2,n3 | ζ2n1,n2,n3 | … | ζHn1,n2,n3 | Value of the h-th order parameter ζh (h=1,2,...,H) at grid point (n1, n2, n3) |

## 2.6. region.in (optional)

Stores an array of the spatial distribution of a weight parameter gr (unitless) arranged in a row-major order, describing the selected real-space region the diffraction of which should be computed. g=0~1, where gr=1 indicates that the spatial point r is fully inside the computed region and gr=0 indicates that the spatial point r is outside the region. A diffuse boundary of the region is allowed by using a finite g with 0<g<1, meaning that the spatial point r is partially inside the computed region with a weight of g. If this file is omitted, the program takes a default region for the diffraction computation and then stores the corresponding gr data in an output file region.00000000.dat. The format of region.in is as follows:

Table 6 Format of the input file region.in

| Data in the file |  |  |  | Explanation |
| --- | --- | --- | --- | --- |
| n1 | n2 | n3 |  | Total number of simulation grids in each direction |
| 1 | 1 | 1 | g1,1,1 | Weight parameter g at grid point (1,1,1) |
| ⋮ |  |  |  | ⋮ |
| 1 | 1 | n3 | g1,1,n3 | Weight parameter g at grid point (1,1,n3) |
| ⋮ |  |  |  | ⋮ |
| 1 | n2 | n3 | g1,n2,n3 | Weight parameter g at grid point (1,n2,n3) |
| ⋮ |  |  |  | ⋮ |
| n1 | n2 | n3 | gn1,n2,n3 | Weight parameter g at grid point (n1, n2, n3) |

# 3. Output files

The program outputs 4 files as follows.

I.00000000.dat

Stores an array of the diffraction intensity Iq (unitless), arranged in a row-major order.

lg_{10}I.00000000.dat

Stores an array of log10Iq (unitless), arranged in a row-major order.

QVector.00000000.dat

Stores an array of the reciprocal space vectors q1, q2, and q3 (nm−1) of the computed diffraction intensity Iq, arranged in a row-major order.

region.00000000.dat

Stores an array of the weight parameter gr (unitless) arranged in a row-major order. For the definition of gr, see Section 2.6. The data follow a same format with those in region.in. This output file is generated only if region.in is not provided.

# References

[1] T. Yang et al. Computing diffraction patterns of microstructures from phase-field simulations. Acta Mater. 239, 118258 (2022).

[2] B.L. Henke, E.M. Gullikson, and J.C. Davis. X-ray interactions: photoabsorption, scattering, transmission, and reflection at E=50-30000 eV, Z=1-92, At. Data Nucl. Data Tables 54, 181 (1993).